## Slide 1: Nemak Group Meeting 2/3/2017

## Slide 2: Topics
HPDC process
Research goals
Present work
Future work

## Slide 3: Why study the HPDC process
Complicated process:
  Rapid filling of mold
  Moderately high pressure (80 Mpa)
  Complicated geometry
  Variable solidification conditions.
Risks:
  Porosity
  Shear banding
  Unwanted microstructure = Coarse needle-like silicon and Fe-rich intermetallics

## Slide 4: Research goals
Acquire data for A383 simulations
Predict macroscale solidification and filling conditions in casting.
  Ansys Fluent
  NovaCast NovaFlow&Solid
Interpolate cooling rates to finer microscale mesh
  Microscale solidification structure simulation using cellular automata

## Slide 5: Present work
Literature review
Novaflow&Solid simulations for solidification conditions
Fluent simulations for solidification conditions
Experimental results on size of eutectic and sludge-phase (Fe-rich intermetallic)

## Slide 6: Fluent steady-state

## Slide 7: Pressure effect on cooling rate
K.A. Batyshev. Casting of Aluminum Alloys with Pressure Crystallization. Part 1, Met Sci Heat Treat+ 53 (2012) 463-471.
Pressure drop for height/diameter in cylindrical casting

## Slide 8: Pressure effect: eutectic temperature Eutectic temperature increases
E. Brosh, G. Makov, R.Z. Shneck. Application of CALPHAD to high pressures, Calphad 31 (2007) 173-185.
J.J. Sobczak, L. Drenchev, R. Asthana. Effect of pressure on solidification of metallic materials, Int J Cast Metal Res 25 (2012) 1-14.
L.V. Nikulin. Crystallization conditions and structure of Al-Si alloys in casting under pressure, Met Sci Heat Treat+ 39 (1997) 384-389.

## Slide 9: Pressure effect: phase diagram Diagram moves up and to the right!
J.J. Sobczak, L. Drenchev, R. Asthana. Effect of pressure on solidification of metallic materials, Int J Cast Metal Res 25 (2012) 1-14.
E. Brosh, G. Makov, R.Z. Shneck. Application of CALPHAD to high pressures, Calphad 31 (2007) 173-185.

## Slide 10: NovaCast NovaFlow&Solid

## Slide 11: Results
Sample | Cooling rate, K/s
1 | 1.7
2 | 1.2
3 | 2.8
4 | 10
5 | 25
Silicon
Sludge

## Slide 12: Conclusions
1. At cooling rate above 2.5 K/s, mean particle size for sludge and silicon dramatically increase
2. Particle size appears to have a logarithmic relationship with simulated solidification time
3. More experimental work is needed to determine the sludge formation mechanism.

## Slide 13: Future work
Microscale simulations
Interpolate solidification conditions from fluent simulations to cellular automata mesh.
Predict microstructure