## Slide 1: Nemak meeting
4/7/2017

## Slide 2: Current goals
Create cycling simulation using Nova Cast
Validate mold surface temperature using FLIR
Validate porosity analysis using CT scan data
Publish paper during Summer

## Slide 3: Cycle info

## Slide 4: Mold surface temperature after 4th cycle, before spray
Simulation max temperature: 523 C
Flir max temperature: 350 C

## Slide 5: Mold surface temperature after 4th cycle, before spray
Flir max temperature: 310 C
Simulation max temperature: 400 C

## Slide 6: Shrinkage simulation
Cycling
No cycling